## Slide 1: Production of a Tube and Box Lab Furnace for 1600 C
ÇINAR ÖNCEL
AHMET BEKİR SOLAK 160713008
BERKAY HOPAL 150713018
YUNUS EMRE ALTAŞ 360713056
SILA İNAN 160713006
MERVE DÖKER 150713023
MERTCAN MUHAMMET AYDIN 150713026
OĞULCAN HAKSEVER 160702035
EVREN KAĞAN GÜRSEL 170702001

## Slide 2: Motivation of Project
The general purpose of the project is to produce a furnace that can be used at any temperature up to 1600 C, which can be both a tube furnace and a box furnace at the same time. In this way, in addition to all the experiments that can be done in the box furnace, it is our goal to commercially produce and promote a new furnace where all the experiments can be done with atmosphere control in the tube furnace can be done. In this way, an economical and space-saving product will be developed for users. When this goal is achieved, a new product that is unique in the market and that we have a patent will be produced.

## Slide 3: Main Parts of the Furnace
Casing
Refractory Materials and Heating elements
Control Panel – Electrical Equipments

## Slide 4: Casing
Casing material is steel
Casing material thickness is 1mm
Dimensions of the furnace;
Height: 800mm
Width: 750mm
Depth: 675mm
Lid thickness: 75mm

## Slide 5: Casing Components
Case of the Furnace
Inner Part
Lid of the Furnace
Alumina Tube
Rail Systems
Control Panel

## Slide 6: Inner Part
The total inner volume of the furnace : 18liters.
4 kinds of materials are used in the interior of the furnace for insulation purposes. These are ceramic board, mullite insulation brick, ceramic fiber blanket and aluminum foil respectively.
The total refractory thickness is 17.5 cm.
Used heating element numbers are 6.

## Slide 8: Lid of the Furnace
Insulation of the lid provided with ceramic board with 10cm total thickness.
2 layers of ceramic board are used.
-Upper layer thickness is 3cm
Bottom layer thickness is 7cm

## Slide 10: Alumina Tube
High purity alumina tube is selected according to the operation temperature and thermal stability. 98%Al2O3 Purity.
Dimensions of the alumina tube
- Length is 1000mm
- Total Radius is 80mm
- Inner Radius is 70mm

## Slide 11: Rail Systems
There are rail systems for easy repair and replacement for the control panel and inner part.

## Slide 12: Technical Drawings of the Furnace

## Slide 15: Used as Box Furnace

## Slide 16: Used as Tube Furnace

## Slide 17: Refractories
One of the purposes of refractory use is to minimize the heat loss of the furnace.
Heat is transmitted by three ways: convection, conduction and radiation. With the refractory materials used , the heat loss caused by conduction and convection can be reduced , but another material is needed to prevent heat loss caused by radiation. Aluminum foil is ideal for this application as it is durable at 600 °C and has reflectivity higher than %90.

## Slide 18: Ceramic Board
Low thermal conductivity
Low heat storage
Excellent thermal shock resistance
Resistant to most chemicals
Easy to cut and shape
Low sound transmission
Resists penetration by molten aluminum and other non-ferrous metals
https://www.northrefractories.com/product-detail/ceramic-fiber-board-high-temperature/

## Slide 19: Mullite Insulation Brick
The refractoriness of the brick can reach temperatures up to 1790 ℃. It is stable at the temperatures up to 1600 ℃ after that point it may start to soften.
https://rsrefractoryfirebrick.com/mullite-insulation-brick/

## Slide 20: Ceramic Fiber Blanket
The thermal conductivity of Ceramic fiber blanket is close to air because it is composed of solid fiber and about 90% porosity. This high amount of porosity destroys the continuity of the solid structure thereby, provides excellent insulation properties.
https://www.ceceramicfiber.com/Products/Ceramicfiberblanket.html

## Slide 21: Heating Element
Molybdenum disilicide (MoSi2) heating elements are resistant heating elements that prevent oxidation of the inner core by forming a compact quartz glass coating on the surface under high temperature. The temperature generated by MoSi2 rises up to 1700-1830 °C in an oxidation atmosphere.
https://www.songshanheating.com/mosi2-u-type/

## Slide 23: Heat Transfer Calculations

## Slide 25: Electrical Components
Thermocouple
Control System
Relay

## Slide 26: Thermocouple
https://www.alibaba.com/product-detail/S-type-platinum-rhodium-thermocouple-WRP_62093460341.html

## Slide 27: Control System
https://www.emkoelektronik.com.tr/tr/urunler/esm-4420

## Slide 28: Relay
https://www.lazimbana.com/ssr-trifaze-solid-state-role-25a-40a-50a-75a-p-2823324

## Slide 29: Circuit Diagram

## Slide 30: Cost

## Slide 31: Conclusion
In conclusion, both box furnace and tube furnace have different abilities and usage areas. In this study, both box furnace and tube furnace investigated seperately and instead of using both furnaces seperately for different purposes, combination of the box and tube furnaces into one compact furnace can provide all the features of the box and tube furnace. Also at the end of the study, because of the compact furnace can be used as both tube and box furnace, there is no need to buy both box furnace and tube furnace seperately. That means cost and occupied area for the furnaces can be saved.